SUPPLEMENTARY DATA

Table S1: Relative crystallinity index (CrL) of untreated cowpea sidestream, alkali-treated followed by bleaching, extruded (with and without alkali) followed by bleaching and commercial cellulose.

| Sample | Crystallinity index CrL (%) |
| --- | --- |
| Untreated Bleached only | 55.65 ± 1.97a 72.32 ± 2.33bc |
| Alkali-treated Bleached alkali-treated | 77.25 ± 0.83d 77.68 ± 0.28d |
| Extruded Bleached extruded | 69.34 ± 0.04b 73.37 ± 0.14c |
| Extruded with alkali Bleached extruded with alkali | 69.49 ± 0.25b 75.22 ± 0.71cd |
| C. cellulose | 88.57 ± 0.14e |

Means followed by standard deviation. Means with different letters in the same column are significantly different (p<0.05).

Figure S1: Diameter size distribution of cellulose fibres extracted with conventional alkali pre-treatment followed by bleaching and extrusion pre-treatment (without and with alkali) followed by bleaching.

Table S2: Thermal stabilities of untreated cowpea sidestream, alkali-treated followed by bleaching, extruded (with and without alkali) followed by bleaching and commercial cellulose.

| Sample | To (°C) | T25 (°C) | T50 (°C) | Tmax (°C) | Residues at 500 °C (%) |
| --- | --- | --- | --- | --- | --- |
| Untreated Bleached only | 263.90 ± 0.21bc 263.99 ± 0.91bc | 299.84 ± 0.22bc 307.07 ± 1.17d | 340.48 ± 0.42c 344.16 ± 0.41d | 338.57 ± 1.20de 348.16 ± 0.16f | 24.22 ± 0.37f 19.48 ± 0.60c |
| Alkali-treated Bleached alkali-treated | 260.74 ± 1.68b 285.42 ± 2.60e | 296.34 ± 1.53ab 316.52 ± 2.14f | 331.53 ± 0.68b 341.28 ± 0.95cd | 318.15 ± 0.40a 340.48 ± 0.91de | 24.62 ± 0.34f 16.32 ± 1.02b |
| Extruded Bleached extruded | 260.34 ± 2.00b 272.11 ± 0.89d | 296.76 ± 0.66ab 311.39 ± 1.31e | 330.80 ± 1.68b 352.04 ± 2.06e | 328.50 ± 3.57bc 360.24 ± 4.24g | 23.09 ± 0.62ef 20.96 ± 0.22cd |
| Extruded with alkali Bleached extruded with alkali | 255.76 ± 0.73a 266.35 ± 0.42c | 292.38 ± 0.68a 301.95 ± 0.20c | 327.09 ± 0.17a 339.35 ± 0.62c | 323.37 ± 1.23ab 333.98 ± 0.16cd | 22.21 ± 0.08de 23.40 ± 0.05ef |
| C. cellulose | 319.44 ± 0.05f | 332.44 ± 1.45g | 341.84 ± 0.05cd | 345.47 ± 2.13ef | 7.01 ± 0.10a |

Means followed by standard deviation. Means with different letters in the same column are significantly different (p<0.05). To is the initial degradation temperature, T25 is the temperature at 25 % mass loss, T50 is the temperature at 50 % mass loss, Tmax is the temperature at maximum degradation.