Photocatalytic Degradation of Efavirenz and Nevirapine using Visible Light-Activated Ag-AgBr-LDH Nanocomposite Catalyst

Lehlogonolo Tabana*, Davy-Rayn Booysens, Shepherd Tichapondwa

Department of Chemical Engineering, Sustainable Environmental and Water Utilisation Processes Division, University of Pretoria, Pretoria, 0028, South Africa.

tabana.ls@tuks.co.za

Supplementary data

Table S1

Positions of the basal planes and crystallite parameters

| Parameter | Sample ID |  |
| --- | --- | --- |
|  | LDH | Ag-AgBr-LDH |
| 2θ (003) (°) | 13.39 | 12.96 |
| 2θ (006) (°) | 26.64 | 26.31 |
| 2θ (009) (°) | 40.36 | 40.37 |
| 2θ (110) (°) | 71.28 | 71.11 |
| d(003) (Å) | 7.67 | 7.92 |
| c (Å) | 23.21 | 23.56 |
| a (Å) | 3.07 | 3.07 |
| L (nm) | 18.26 | 14.09 |

Fig. S1. XRD spectra for Ag-AgBr-LDH photocatalyst.

Fig. S2. Point of zero charge for various photocatalyst.

Fig. S3. PFO kinetics model fittings for efavirenz and nevirapine (5 mg/L).

Fig. S4. PFO kinetics model fittings for efavirenz and nevirapine (20 mg/L).