# Electronic Supplementary Information (ESI)

# for

# Natural acids as catalysts for the continuous flow production of the green solvent 2,2,5,5-tetramethyltetrahydrofuran

Bernice M. Curriea, Estefan van Vuurena, Jaimee Jugmohanb, Jenny-Lee Panayidesb, and Darren L. Rileya*

Department Chemistry, University of Pretoria, Pretoria, 0028, South Africa;

Pharmaceutical Technologies, Chemicals cluster, CSIR, Pretoria campus, Pretoria, 0001, South Africa;

Correspondence: Darren.riley@up.ac.za; Tel.: +2712-420-3097

Table of contents

1.	Experimental	2

1.1	General experimental detail	2

1.2	Flow reactors and equipment	2

1.3	Characterisation and purification	3

1.4	Setup for synthesis of TMTHF	5

1.5	Space-time yield and throughput calculations	5

2.	Additional data related to main article	5

2.1	GC-FID conversions for catalyst screening of various natural acids, showing byproduct percentage	5

2.2	DoE results using citric acid monohydrate	6

2.3	Results for co-catalyst approach	8

2.4	Results for further optimization at various temperatures and residence times	8

2.5	Cost analysis details	9

2.6	Summary of CHEM21 Metrics toolkit (Please refer to Excel spreadsheet for full calculations)	10

2.7	TMTHF Price commercially available	10

3.	Experimental section	16

3.1	2,5-Dimethyl-2,5-hexanediol 2 (Starting Material)	16

3.2	2,2,5,5-tetramethyltetrahydrofuran (TMTHF) 1:	16

4.	GC-FID Method Information	19

4.1	GC-FID method details	19

4.2	GC-FID standard curve	20

5.	Characterization data	24

5.1	Byproduct formation according to Byrne and co-workers1–5	24

5.2	Nuclear magnetic resonance spectra	25

5.3	Fourier transform infrared spectra	31

5.4	HRMS Spectra	33

6.	References	33

## Experimental

### General experimental detail

All batch reactions were carried out using traditional chemistry methods, glassware and apparatus found in a standard synthetic laboratory. Batch distillations were performed using a Dean-Stark apparatus. Before use, all glassware was oven- or flame-dried. Ethyl acetate was used for GC analysis and distilled from calcium hydride. Water was obtained from the tap and filtered using gravity filtration. 2,5-Dimethyl-2,5-hexanediol was purchased from Sigma-Merck and Fluorochem, and a H-Beta Zeolite sample was supplied from Clariant. All starting materials and solvents were used without purification. The solvent removal was performed under reduced pressure (approximately 20 mmHg) using a standard Heidolph rotary evaporator at temperatures between 40 °C and 90 °C, when using ethyl acetate.

### Flow reactors and equipment

- Flow reactor:

  - UniqsisTM Binary Pump Module (BPM) reactor equipped with 10 mL HPLC pump heads

  - The reactor was fitted with standard 1.0 mm inner diameter or 1.5 mm inner diameter PTFE or SS tubing.

- Coil reactors:

  - Stainless-steel coil reactors had a maximum operating temperature of 260 °C and maximum pressure of 1000-psi (70 bar) with volumes of 2.5, 5, and 20 mL (1.0 mm inner diameter) and 40 mL (2.1 mm inner diameter)

- The coil reactors were heated using a UniqsisTM HotCoil flow module with an operational temperature range from ambient temperature to 260 °C. A UniqsisTM Polar Bear PLUS flow module, which has an operational temperature range of -40 °C to 150 °C, was used for cooling.

- Static mixer:

  - A 0.5 mL (3.2 mm internal diameter) VapourtecTM static mixer with a maximum pressure rating of 362-psi (25 bar) was used.

- Cartridge-based back-pressure regulators (BPR) were used, with pressures set to 10 bar based on application. They were fitted with chemically resistant perfluoro polymer components.

### Characterisation and purification

- Purification: Isolated yields were obtained from distillation using Dean-Stark, insulated with cotton wool and foil.

- Nuclear Magnetic Resonance (NMR)was performed using a Bruker Ultrashield AVANCE-III spectrometer.

  - Splitting and multiplicity patterns are reported as singlet (s), doublet (d), doublet of doublet (dd), triplet (t), doublet of triplet (dt), quartet (q), multiplet (m), and broad singlet (bs). Coupling constants, J, were reported in Hertz (Hz). Chemical shifts δ are reported in parts per million (ppm).

  - 1H NMR spectra were recorded at 300 and 400 MHz, and chemical shifts were reported in the following order: chemical shift (δH, ppm); coupling constants (J, Hz); multiplicity; number of protons; proton assignment, and all signals are referenced relative to deuterated chloroform (CDCl3) at 7.27 ppm.

  - 13C NMR were recorded at 75MHz and 101 MHz and chemical shifts were reported in the following order: chemical shift (δC, ppm); assignment and all signals are referenced relative to CDCl3 at 77.36 ppm.

  - Both 1H NMR and 13C NMR were processed using MestreNova 12.0 as follows:

    - Apodization: 			0.10 Hz

    - Zero Filling and LP:		262144 (256 K)

    - Auto Baseline Correction:	Polynomial fit (5th order)

  - qHNMR calculations:

    - QNMR samples were prepared using anisole (99%) as internal standard (I.S) and the targeted compound (T) dissolved in 600 µL deuterated chloroform, and the conversion was calculated as follows:

% Conversion=I.S protons×T  Integral×T MW×I.S (Mass)T protons×I.S Integral×I.S MW×T Mass ×% I.S Purity Percentage

- Fourier-transform Infrared (FTIR) spectroscopy was performed on a JASCO FT/IR-4X spectrometer instrument.

  - Functional group signals were reported as wavenumbers (cm−1) ranging from 400 – 3000 cm-1.

- GC-FIC was performed with a Shimadzu GC-2010 instrument, which has an FID detector and an InertCap5MS column (0.25 um (film thickness), 30 m (column length), 0.25 mm ID, and a max temperature of 320 °C).

  - The injection volume was set to 1.0 µL with injection mode using split ratio of 30:1 and Helium as carrier gas

  - Samples were prepared using distilled ethyl acetate to approximate concentrations relating to each method.

- High-resolution mass spectra (HRMS) were recorded on a Waters Synapt G2 Mass Spectrometer at 70 eV and 200 mA.

  - For analysis, the instrument was operated under the following conditions: a capillary voltage of 2.8 kV (positive mode), a sampling cone (ramped from 20 V – 40 V), an extraction cone of 4 V, a source temperature of 100 °C, a desolvation temperature of 200 °C, cone gas of 100 L.h-1, desolvation gas of 500 L.h-1, inert gas source: nitrogen.

  - Samples were prepared in analytical grade acetonitrile to an approximate concentration of 10 μg.mL-1.

- Nomenclature

  - The compounds were named according to IUPAC nomenclature, using ChemDraw Ultra 12.0. Numbering was chosen as a matter of convenience.

- Referencing

  - All sources were cited with Mendeley Reference Manager, using the Royal Society of Chemistry (with titles) citation style.

### Setup for synthesis of TMTHF

| Figure 1: Batch setup using Dean-Stark apparatus | Figure 2: Flow setup for the 200-gram scale |
| --- | --- |
| Figure 3: Flow collection flask showing separation prior to liquid-liquid extraction (TMTHF at the top) | Figure 4: Distillation setup for the 200-gram scale |

### Space-time yield and throughput calculations

| Yield | Residence time | Coil volume | Collection time |
| --- | --- | --- | --- |
| 125.697 grams = 0.125697 kg | 20 min = 0.333 hours | 40 mL = 0.040 L | 15 hours 15 min = 15.25 hours |
| Formula |  | Calculation | Answer |
| Throughput (g.h-1) | yield (grams)collection time (hours) | 125.697 grams15.25 hours | 8.2424 g h-1 |
| Space-time yield (kg h-1 L-1) | yield (grams)residence time hours×reactor volume (L) | 0.125697 kg0.333 hours ×0.04 L | 9.4272 kg h-1 L-1 |

## Additional data related to main article

### TMTHF Price commercially available

| Supplier | Purity | Quantity | Price | Last updated date |
| --- | --- | --- | --- | --- |
| - Accel Scientific S.L. (Spain) | 95% | 100 mg | 52 EUR | 2025-06-10 |
|  | 95% | 250 mg | 77 EUR |  |
|  | 99% | 500 mg | 97 EUR |  |
|  | 95% | 1 g | 155 EUR |  |
|  | 95% | 5 g | 372 EUR |  |
| - Bio-Farma Ltd. (United Kingdom) | Not specified | 1 g | 452 GBP | 2025-06-05 |
|  |  | 5 g | 1093 GBP |  |
|  |  | 10 g | 1595 GBP |  |
| - Sigma Aldrich, Inc. (USA) | 95% | 100 mg | 166.25 AUD | 2025-06-02 |
|  |  |  | 18200 JPY |  |
|  |  |  | 52.9 USD |  |
|  |  |  | 91.98 GBP | 2025-02-21 |
|  |  |  | 94.05 CHF |  |
|  |  |  | 2351.25 CZK |  |
|  |  |  | 705.38 DKK |  |
|  |  |  | 94.05 EUR |  |
|  |  |  | 35739 HUF |  |
|  |  |  | 1081.58 NOK |  |
|  |  |  | 423.23 PLN |  |
|  |  |  | 1072.17 SEK |  |
|  | 95% | 250 mg | 211.88 AUD | 2025-06-02 |
|  |  |  | 23200 JPY |  |
|  |  |  | 79.35 USD |  |
|  |  |  | 113.04 GBP | 2025-02-21 |
|  |  |  | 121.65 CHF |  |
|  |  |  | 3041.25 CZK |  |
|  |  |  | 912.38 DKK |  |
|  |  |  | 121.65 EUR |  |
|  |  |  | 46227 HUF |  |
|  |  |  | 1398.98 NOK |  |
|  |  |  | 547.43 PLN |  |
|  |  |  | 1386.81 SEK |  |
|  | 95% | 500 mg | 155.16 GBP | 2025-02-21 |
|  | 95% | 1 g | 358.68 AUD | 2025-06-02 |
|  |  |  | 39600 JPY | 2025-02-21 |
|  |  |  | 164.45 USD |  |
|  |  |  | 187.92 GBP |  |
|  |  |  | 206.75 CHF |  |
|  |  |  | 5168.75 CZK |  |
|  |  |  | 1550.63 DKK |  |
|  |  |  | 206.75 EUR |  |
|  |  |  | 78565 HUF |  |
|  |  |  | 2377.63 NOK |  |
|  |  |  | 930.38 PLN |  |
|  |  |  | 2356.95 SEK |  |
|  | 95% | 2.5 g | 266.31 GBP | 2025-02-21 |
|  | 95% | 5 g | 795.1 AUD | 2025-06-02 |
|  |  |  | 88200 JPY |  |
|  |  |  | 417.45 USD |  |
|  |  |  | 396.18 GBP | 2025-02-21 |
|  |  |  | 443.65 CHF |  |
|  |  |  | 11091.2 CZK |  |
|  |  |  | 3327.38 DKK |  |
|  |  |  | 443.65 EUR |  |
|  |  |  | 168587 HUF |  |
|  |  |  | 5101.98 NOK |  |
|  |  |  | 1996.43 PLN |  |
|  |  |  | 5057.61 SEK |  |
|  | 95% | 10 g | 657.09 GBP | 2025-02-21 |
| - AA Blocks LLC (USA) | 95% | 100 mg | 37 USD | 2025-05-31 |
|  |  | 250 mg | 55 USD |  |
|  |  | 1 g | 113 USD |  |
|  |  | 5 g | 287 USD |  |
| - Ambeed Inc. (USA) | 95% | 100 mg | 100 mg | 2025-05-28 |
|  |  | 250 mg | 60 USD |  |
|  |  | 1 g | 120 USD |  |
|  |  | 5 g | 290 USD |  |
| - AK Scientific Inc. | 95% | 100 mg | 169 USD | 2025-05-08 |
|  |  | 250 mg | 285 USD |  |
|  |  | 1 g | 766 USD |  |
|  |  | 5 g | 2684 USD |  |
| - Apollo Scientific Ltd. (United Kingdom) | 99% | 100 mg | 60 GBP | 2025-05-08 |
|  |  | 250 mg | 89 GBP |  |
|  |  | 1 g | 183 GBP |  |
|  |  | 5 g | 663 GBP |  |
| - Envigen Pharmaceuticals Inc. (USA) | 97% | 100 mg | 167 USD | 2025-05-05 |
|  | 95% | 100 mg | 167 USD | 2025-03-10 |
|  | 97% | 250 mg | 249 USD | 2025-05-05 |
|  | 95% | 250 mg | 249 USD | 2025-03-10 |
|  | 97% | 1 g | 577 USD | 2025-05-05 |
|  | 95% | 1 g | 577 USD | 2025-03-10 |
| - Key Organics Ltd. (United Kingdom) | >95percent | 100 mg | 235 GBP | 2025-05-01 |
|  |  | 250 mg | 328 GBP |  |
|  |  | 1 g | 698 GBP |  |
| - Aladdin Scientific Corporation (USA) | >=95percent | 100 mg | 363.9 USD | 2025-04-29 |
|  |  |  | 349.34 EUR |  |
|  |  | 250 mg | 576.9 USD |  |
|  |  |  | 553.82 EUR |  |
|  |  | 500 mg | 390.9 USD |  |
|  |  |  | 375.26 EUR |  |
|  |  | 1 g | 692.9 USD |  |
|  |  |  | 665.18 EUR |  |
|  | >=90percent | 1 g | 650.9 USD |  |
|  |  |  | 624.86 EUR |  |
|  | >=95percent | 5 g | 2251.9 USD |  |
|  |  |  | 2161.82 EUR |  |
|  | >=90percent |  | 2149.9 USD |  |
|  |  |  | 2063.9 EUR |  |
| - ChemScene LLC (USA) | 98% | 100 mg | 148 USD | 2024-09-09 |
|  |  | 250 mg | 64 USD | 2025-04-23 |
|  |  | 1 g | 131 USD |  |
|  |  | 5 g | 318 USD |  |
| - Advanced ChemBlocks Inc | 95% | 1 g | 120 USD | 2025-04-22 |
|  |  | 5 g | 290 USD |  |
|  |  | 25 g | 780 USD |  |
| - AstaTech Inc. (USA) | 95% | 100 mg | 214 USD | 2025-04-17 |
|  |  | 250 mg | 365 USD |  |
|  |  | 1 g | 730 USD |  |
| - Georganics Ltd. (Europe) | 97% | 200 g | price on demand | 2025-04-11 |
| - Chemenu Inc. (China) | 95% | 100 mg | 154 USD | 2025-04-09 |
|  |  | 250 mg | 259 USD |  |
|  |  | 1 g | 697 USD |  |
|  |  | 5 g | 2441 USD |  |
| - SynHet (Lithuania) | >96percent+ | upon inquiry | upon inquiry | 2025-04-04 |
| - Combi-Blocks Inc. (USA) | 97% | 100 mg | 40 USD | 2025-04-02 |
|  |  | 250 mg | 60 USD |  |
|  |  | 1 g | 290 USD |  |
|  |  | 10 g | 550 USD |  |
| - Biosynth (United Kingdom) | >=95percent | 50 mg | 217 USD | 2025-04-01 |
|  |  | 100 mg | 369 USD |  |
|  |  | 250 mg | 740 USD |  |
| - 1Click Chemistry Inc (USA) | 96% | 100 mg | 44.16 USD | 2025-03-25 |
|  |  | 250 mg | 62.4 USD |  |
|  |  | 500 mg | 98.88 USD |  |
|  |  | 1 g | 126.72 USD |  |
|  |  | 2.5 g | 194.88 USD |  |
|  |  | 5 g | 306.24 USD |  |
|  |  | 10 g | 530.88 USD |  |
|  |  | 25 g | 1134.45 USD |  |
| - Aurum Pharmatech LLC (USA) | 96% | 100 mg | 43.7 USD | 2025-03-25 |
|  |  | 250 mg | 61.75 USD |  |
|  |  | 500 mg | 97.85 USD |  |
|  |  | 1 g | 125.4 USD |  |
|  |  | 2.5 g | 192.85 USD |  |
|  |  | 5 g | 303.05 USD |  |
|  |  | 10 g | 525.35 USD |  |
|  |  | 25 g | 1122.63 USD |  |
|  |  | 50 g | 2163.25 USD |  |
|  |  | 100 g | 4199.33 USD |  |
| - AAA Chemistry (USA) | 95% | upon inquiry | upon inquiry | 2025-03-20 |
| - BLD Pharmatech Ltd. (China) | 95% | 100 mg | 46 USD | 2025-03-20 |
|  |  |  | 46 EUR |  |
|  |  | 250 mg | 69 USD |  |
|  |  |  | 68 EUR |  |
|  |  | 1 g | 143 USD |  |
|  |  |  | 139 EUR |  |
|  |  | 5 g | 363 USD |  |
|  |  |  | 337 EUR |  |
| - ChemPUR Feinchemikalien und Forschungsbedarf GmbH (Germany) | 95% | upon inquiry | upon inquiry | 2025-03-04 |
| - RR SCIENTIFIC LLC | 97percent+ | 100 mg | 168 USD | 2025-03-03 |
|  |  | 250 mg | 250 USD |  |
|  |  | 1 g | 562 USD |  |
|  | 98% | 1 g | 2167.66 USD | 2024-07-11 |
|  | 95% | 1 g | 132 USD | 2025-03-03 |
| - Enamine (Ukraine) | 95% | 5 g | 319 USD | 2025-03-01 |
|  |  | 10 g | 553 USD |  |
| - Appchem (Hong Kong) | 99% | 100 mg | 50 USD | 2025-02-15 |
|  | 95% | 250 mg | 79 USD |  |
|  | 99% | 500 mg | 110 USD |  |
|  |  | 1 g | 146 USD |  |
|  |  | 5 g | 361 USD |  |
| - Ambinter (France) | >90percent | upon inquiry | upon inquiry | 2025-02-13 |
| - XtalpI Inc. (USA) | 95% | 100 mg | upon inquiry | 2025-02-11 |
| - 1Pluschem LLC (USA) | 97% | 100 mg | 71 USD | 2025-01-23 |
|  |  | 250 mg | 156 USD |  |
|  |  | 5 g | 229 USD |  |
| - Activate Scientific (Germany) | 95% | 250 mg | 185 USD | BOC Sciences |
|  |  | 1 g | 404 USD |  |
|  |  | 5 g | 1248 USD |  |
| - BOC Sciences | 98% | upon inquiry | upon inquiry | 2024-12-18 |
| - Hangzhou Yuhao Chemical Technology Co., Ltd. (China) | Not specified | upon inquiry | price on askingv | 2024-10-24 |
| - 10X CHEM (USA) | 97% | 100 mg | 70 USD | 2024-09-06 |
|  |  | 250 mg | 99 USD |  |
|  |  | 1 g | 276 USD |  |
|  |  | 5 g | 810 USD |  |
|  |  | 10 g | 1198 USD |  |
| - Aaron Chemicals LLC (USA) | 95% | 100 mg | 27 USD | 2024-08-08 |
|  |  | 250 mg | 61 USD |  |
|  |  | 1 g | 189 USD |  |
|  |  | 5 g | 712 USD |  |
| - Angene International Ltd. (China) | 95% | 100 mg | 27 USD | 2024-07-26 |
|  |  | 250 mg | 59 USD |  |
|  |  | 1 g | 194 USD |  |
|  | 99percent;RG | 5 g | 762 USD |  |
| - Manchester Organics Ltd. (United Kingdom) | Not specified | upon inquiry | upon inquiry | 2024-07-25 |
| - Shanghai Sunway Pharmaceutical Technology Co., Ltd. (China) | 97% | 1 g | 645 USD | 2024-05-08 |
| - eMolecules, Advanced ChemBlocks Inc. (USA) | 95% | 1 g | 168 USD | 2024-02-01 |
|  |  | 5 g | 406 USD |  |
|  |  | 25 g | 1092 USD |  |
| eMolecules, Ambeed Inc. (USA) | 95% | 100 mg | 198 USD | 2024-02-01 |
|  |  | 250 mg | 334 USD |  |
|  |  | 1 g | 895 USD |  |
|  |  | 5 g | 3132 USD |  |
| eMolecules, AstaTech Inc. (USA) | 95% | 100 mg | 275 USD | 2024-02-01 |
|  |  | 250 mg | 426 USD |  |
|  |  | 1 g | 852 USD |  |
| eMolecules, Bio-Farma Ltd. (USA) | Not specified | 1 g | 631 USD | 2024-02-01 |
|  |  | 5 g | 1520 USD |  |
|  |  | 10 g | 2161 USD |  |
| eMolecules, Biosynth (USA) | Not specified | 50 mg | 187 USD | 2024-02-01 |
|  |  | 100 mg | 317 USD |  |
|  |  | 250 mg | 634 USD |  |
| eMolecules, BLD Pharmatech GmbH (USA) | 95% | 100 mg | 166 USD | 2024-02-01 |
|  |  | 250 mg | 280 USD |  |
|  |  | 1 g | 754 USD |  |
|  |  | 5 g | 2636 USD |  |
| eMolecules, BLD Pharmatech Ltd. (USA) | 95% | 100 mg | 202 USD | 2024-02-01 |
|  |  | 250 mg | 341 USD |  |
|  |  | 1 g | 917 USD |  |
|  |  | 5 g | 3209 USD |  |
| eMolecules, Combi-Blocks Inc. (USA) | 97% | 100 mg | 98 USD | 2024-02-01 |
|  |  | 250 mg | 140 USD |  |
|  |  | 1 g | 392 USD |  |
|  |  | 5 g | 1155 USD |  |
|  |  | 10 g | 1708 USD |  |
| eMolecules, Key Organics Ltd. (USA) | 95% | 100 mg | 553 USD | 2024-02-01 |
|  |  | 250 mg | 771 USD |  |
|  |  | 1 g | 1644 USD |  |
| eMolecules, Toronto Research Chemicals (USA) | Not specified | 50 mg | 132 USD | 2024-02-01 |
|  |  | 100 mg | 175 USD |  |
|  |  | 500 mg | 696 USD |  |
| eMolecules, WuXi AppTec (USA) | Not specified | 100 mg | 181 USD | 2024-02-01 |
|  |  | 250 mg | 287 USD |  |
| - ArrakisTek Inc. (USA) | 95% | upon inquiry | price on demand | 2024-01-17 |
| - Fluorochem Ltd. (United Kingdom) | 95% | upon inquiry | upon inquiry | 2023-10-02 |
| - Chemieliva Pharmaceutical Co., Ltd. | 98% | 1 g – 50 kg | Not specified | 2023-07-19 |
| - Hong Kong Chemhere Co., Ltd. (China) | Not specified | Not specified | Not specified | 2021-05-11 |
| - Aurora Fine Chemicals LLC (USA, Austria) | 95-98percent | upon inquiry | Price on request | 2021-04-20 |
| - Debye Scientific Co., Ltd. | 95% | 5 g – 500 g | POA | 2020-01-17 |

CAS no: 15045-43-9 all prices on the 11th of August 2025 from Reaxys https://www-reaxys-com.uplib.idm.oclc.org/#/results/substances/20/RX001_1107353758479105994/UlgwMDE9Uw==/list/1f46ad0c-210b-4494-9b9c-3a060d6bec87/1/asc/IDE.RCSID

### GC-FID conversions for catalyst screening of various natural acids, showing byproduct percentage

Table 1:  Screening of initial flow experiments of various natural acid catalysts showing byproduct formation

| Catalyst Name | GC-FID Conversions (%) |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | 100 °C |  | 140 °C |  |  |  |
|  | 20 minutes | 40 minutes | 20 minutes | Byproduct % | 40 minutes | Byproduct % |
| Acetic acid | 0.17 | 0.27 | 2.88 | 26.90 | 7.44 | 5.30 |
| Ascorbic acid | 0.10 | 0.35 | 11.11 | 5.10 | 22.70 | 0.28 |
| CAM | 0.77 | 1.10 | 35.34 | 1.34 | 28.22 | 1.73 |
| Formic acid | 0.75 | 1.71 | 32.49 | 6.65 | 22.54 | 8.73 |
| Gallic acid | 0.21 | 0.36 | 4.00 | 13.46 | 4.46 | - |
| Lactic acid * | 0.54 | 0.35 | 21.41 | 8.50 | 19.63 | 1.63 |
| L-Mandelic acid | 0.57 | 0.47 | 25.68 | 2.97 | 35.62 | 0.08 |
| Maleic acid | 3.73 | 6.93 | 37.30 | 2.47 | 27.60 | 1.50 |
| Malonic acid | 1.43 | 2.72 | 9.00 | 5.01 | 30.08 | 5.75 |
| Nicotinic acid | 0.21 | 0.39 | 7.93 | - | 18.46 | 10.52 |
| Oxalic acid | 6.75a | 7.46b | 41.81 | 2.25 | 33.06 | 6.2 |
| Picolinic acid | 0.22 | 0.15 | 9.39 | 10.26 | 9.49 | 8.72 |
| Succinic acid | 0.31 | 1.29 | 19.83 | 4.90 | 20.62 | 5.15 |
| D-tartaric acid salt | 0.28 | 0.22 | 2.10 | - | 1.40 | - |
| DL-Tartaric acid | 1.73 | 3.55 | 35.03 | 0 | 28.87 | 0.05 |

a byproduct: 1.37% ; b byproduct: 1.41%. Byproduct percentage determined by GC-FID conversions based on standard curve; * 90 % Lactic acid solution

### DoE results using citric acid monohydrate

| Figure 5: Representation of replicate plot that demonstrates the variation between results within the experimental limits | Figure 6: Representation of a coefficient plot illustrating essential terms and their interactions |
| --- | --- |
| Figure 7: Representation of a summary of fit plot demonstrating the reliability and validity of the model | Figure 8: Representation of the observed vs. predicted plot for the results based on a line of best fit |

### Results for co-catalyst approach

Table 2: Co-catalyst reactions using CAM (0.10 equiv.) at 0.50 M concentration using a 316L Stainless steel coil (40 mL) and cooling coil (2.5 mL) at 15°C.

| Entry no | Catalyst combination with CAM (0.10 equivalents) | Cat Equiv. | Tres. (min) | Temp. (°C) | GC-FID Conv. |
| --- | --- | --- | --- | --- | --- |
| 1 | Tartaric acid | 0.10 | 10 | 120 | 9.32 |
| 2 | Tartaric acid | 0.10 | 10 | 120 | 8.64 |
| 3 | Oxalic acid | 0.05 | 20 | 140 | 25.73 |
| 4 | Oxalic acid | 0.05 | 20 | 160 | 33.19 |
| 5 | Oxalic acid | 0.05 | 15 | 140 | 28.41 |
| 6 | Oxalic acid | 0.05 | 15 | 160 | 31.16 |
| 7 | Tri-sodium citrate | 0.10 | 20 | 140 | 1.09 |
| 8 | Ammonium acetate | 0.10 | 20 | 140 | 2.15 |
| 9 | Tri-ammonium citrate | 0.10 | 20 | 140 | 0.62 |

### Results for further optimization at various temperatures and residence times

Table 3: GC-FID conversions using citric acid monohydrate (0.10 equiv.) at 0.50 M concentration and screening coil volume, residence times and temperature

| Entry no | Tres. (min) | Coil Volume (mL) | Temp. (°C) | GC-FID Conv. |
| --- | --- | --- | --- | --- |
| 1 | 10 | 20 | 100 | 1.23 |
| 2 | 20 | 20 | 100 | 2.35 |
| 3 | 10 | 20 | 120 | 13.06 |
| 4 | 20 | 20 | 120 | 15.52 |
| 5a | 15 | 20 | 100 | 1.93 |
| 6a | 30 | 20 | 100 | 6.22 |
| 7a | 15 | 20 | 120 | 8.55 |
| 8a | 30 | 20 | 120 | 5.64 |
| 9 | 10 | 20 | 140 | 24.06 |
| 10 | 20 | 20 | 140 | 21.87 |
| 11 | 10 | 20 | 160 | 18.28 |
| 12 | 20 | 20 | 160 | 8.49 |
| 13 | 20 | 40 | 120 | 12.91 |
| 14 | 40 | 40 | 120 | 22.31 |
| 15 | 15 | 40 | 140 | 24.9 |
| 16b | 20 | 40 | 140 | 33.44 |
| 17c | 20 | 40 | 140 | 34.17 |
| 18 | 30 | 40 | 140 | 31.7 |
| 19 | 60 | 40 | 140 | 7.44 |
| 20 | 5 | 5 | 180 | 37.88 |
| 21 | 5 | 5 | 200 | 33.29 |

a Performed Vapourtec Rapid Mixing coil (20 mL, 3.2 mm I.D); b recycled once; c recycled twice.

### Cost analysis details

Figure 9: Diagrammatic representation of the mass distribution when producing TMTHF using citric acid monohydrate

Figure 10: Diagrammatic representation of the cost distribution when producing TMTHF using citric acid monohydrate

### Summary of CHEM21 Metrics toolkit (Please refer to Excel spreadsheet for full calculations)

Table 4: Additional assessment by CHEM21 metric toolkit and techno economics for zeolite and citric acid monohydrate approaches to synthesize TMTHF 1

| Category | Zeolite approach1 | Citric acid monohydrate approach |
| --- | --- | --- |
| Solvent | No solvent | Water |
| Catalyst/Enzyme/ Stoichiometric reagent | Catalyst | Catalyst |
| Catalyst/Enzyme recovery | Recoverable | Recoverable and biodegradable |
| Critical elements | Al (Zeolite) | None (citric acid monohydrate) |
| Reaction temperature | 130 | 140 |
| Reflux/>5 °C below reflux | n/a | n/a |
| Work up | Distillation (115 °C) | Distillation (115 °C) |
| EHS (worst) | None | H319, H335 |

## Experimental section

### 2,5-Dimethyl-2,5-hexanediol 2 (Starting Material)

GC-FID retention time: 5.59 min, 1H NMR (400 MHz, Chloroform-d) δ 2.67 – 2.50 (m, 2H, H3 & H7), 1.53 (s, 4H,H4 & H5 ), 1.19 (s, 12H, H1 & H8-10), 13C NMR (101 MHz, CDCl3) δ 77.38, 77.06, 76.74, 70.57 (C2 & C6), 37.76 (C4-5), 29.40 (C1 & C8-10); IR Vmax/cm-1 3270.68 (O-H stretch), 2967.9 (C-H stretch), 2869.56, 1470.46 (C-H bend), 1414.53, 1285.32, 1246.75, 1199.51, 1140.69, 1096.33, 965.198(C-O bond), 905.415, 752.102, 680.749.

### 2,2,5,5-tetramethyltetrahydrofuran (TMTHF) 1:

#### Batch method using H-beta Zeolite

2,5-Dimethyl-2,5-hexanediol 2 (10.00 g, 68.41 mmol, 1.0 equiv.) was heated and stirred until molten (100 °C ). H-Beta zeolite (22.8 mg, 0.14 mmol, 0.002 equiv., 0.21 mol %) was added and heated for 4 hours at 130 °C using a Dean-Stark apparatus. The product formed as two layers, the top organic layer was dried over magnesium sulphate and distilled again to obtain 95.0 % isolated yield (8.33 grams, 64.99 mmol, >99% GC-FID conversion, 97,02 % qNMR) of 2,2,5,5-tetramethyltetrahydrofuran (TMTHF) 1 as a clear liquid. GC-FID retention time: 3.06 min 1H NMR (400 MHz, Chloroform-d) δ 1.77 (s, 4H, H2 & H3), 1.18 (s, 9H, H5-8), 13C NMR (101 MHz, CDCl3) δ 80.91(C1 & C4), 77.48, 77.16, 76.84, 38.80 (C2 & C3), 29.77 (C5-8)., IR Vmax/cm-1  2967.91(C-H stretch), 2930.31, 2897.52, 1458.89 (C-H bend), 1375.96, 1364.39, 1308.46, 1264.11, 1205.29, 1142.62, 1078.01, 984.482 (C-O bond), 886.131, 848.525.

#### Batch method using citric acid monohydrate

2,5-Dimethyl-2,5-hexanediol 2 (10.00 g, 68.41 mmol, 1.0 equiv.) was added to water (1.0 M) heated and stirred until molten (100 °C). Citric acid monohydrate (1.44 mg, 6.84 mmol, 0.1 equiv., 10 mol %) was added and heated for 8 hours at 115 °C using a Dean-Stark apparatus. The matrix separated as two layers, the top organic layer was dried over magnesium sulphate and distilled again to obtain 41.8 % isolated yield (3.67 grams, 28.60 mmol, 47.72% GC-FID conversion, 49.03% qNMR ) of  2,2,5,5-tetramethyltetrahydrofuran (TMTHF) 1 as a clear liquid. GC-FID retention time: 3.05 min.

#### Flow method using citric acid monohydrate

##### Preparation of stock solution using citric acid monohydrate

Main article (Table 3, Entry 17): 0.75 M stock solution was prepared by dissolving 2,5-dimethyl-2,5-hexanediol 2 (54.7084 g, 374.13 mmol, 1.0 equiv.) and citric acid monohydrate 3 (7.8746 g, 0.037 mmol, 0.10 equiv.) in water to a total volume of 500 mL. For the 200-gram scale, a 0.75 M stock solution was prepared by dissolving 2,5-dimethyl-2,5-hexanediol 2 (200.356 g, 1370,14 mmol, 1.0 equiv.) and citric acid monohydrate 3 (28.79 g, 137,03 mmol, 0.10 equiv.) in water to a total volume of 1830 mL.

##### UniqsisTM binary pump reactor setup and description for 200-gram scale (Main article: Scheme 3)

The UniqsisTM binary pump reactor was used with a 40 mL (2.10 mm inner diameter) coil. A total flow rate of 2.00 mL min-1 was used to introduce 1830 mL of the stock reservoir into the flow system. Water was used as a pushing solvent. The solution was pumped through a static mixer at room temperature, a coil reactor held at 140 °C (TRes = 20 min), and a 7.5 mL cooling coil held at 20 °C with a 10-bar BPR. The solution was collected and directly extracted using liquid-liquid extraction, after which GC-FID analysis was performed. The TMTHF was isolated via distillation to obtain a 71.6% isolated yield (125.70 grams, 980.40 mmol, >99% GC-FID conversion, 94.16% qNMR ) of  2,2,5,5-tetramethyltetrahydrofuran (TMTHF) 1 as a clear liquid. GC-FID retention time: 3.07 min, 1H NMR (400 MHz, Chloroform-d) δ 1.77 (s, 4H, H2 & H3), 1.17 (s, 12H, H5-8), 13C NMR (101 MHz, CDCl3) δ 80.90 (C1 & C4), 77.48, 77.16, 76.84, 38.79 (C2 & C3), 29.76(C5-8),IR Vmax/cm-1 2967.91 (C-H stretch), 2930.3, 2872.45, 1458.89 (C-H bend), 1375.96, 1364.39, 1308.46, 1264.11, 1205.29, 1142.62, 1078.01, 984.482 (C-O bond), 886.131, 848.525, 767.53, 489.831, HRMS m/z (ES+) 128.1210 [M]+ (C8H16O requires 128.2120 g/mol).

Analysis of TMTHF 1 corresponded with literature results obtained F. Patrick Byrne and co-workers.1-2

## GC-FID Method Information

### GC-FID method details

| Parameter | Setting |
| --- | --- |
| Instrument | Shimadzu GC-2010 instrument with a FID detector |
| Column | InertCap5MS , 0.25 um (film thickness), 30 m (column length), 0.25 mm ID, max temperature 320 °C |
| Carrier Gas | Helium |
| Injection Mode | split ratio was 30:1 |
| Injector Temperature | 250 °C |
| Injection Volume | 1.0 ul |
| Oven Temperature Program | 60 °C for 0.30 minute, 20 °C/min ramp to 140 °C, hold for 1 minute, 50 °C/min ramp to 250 °C, hold for 0.30 minute |
| FID Temperature | 250 °C |
| Air Flow | 400 mL/min |
| Hydrogen Flow | 40 mL/min |
| Sampling rate | 40 msec |
| Makeup Gas (Helium) | Helium (30 mL/min) |
| Run Time | 7.80 min |
| Retention time | TMTHF 1 (3.05 min), Decane (4.81 min), 2,5-Dimethyl-2,5-hexanediol 2 (5.59 min) |
| Internal Standard | Decane (>99%) |
| GC-FID standard curve equation (conducted in triplicates) | y=112.26x |
| R2 value for standard curve | 0.9996 |

### GC-FID standard curve

#### General procedure for preparing concentrations for standard curve

Purified TMTHF (97,02 % conversion using qNMR) was used and several concentrations were prepared in triplicates with the addition of Decane (Density:0.73, 5840 ppm) as an internal standard. A 8 µl aliquot of decane was dispensed directly into an GC vial and diluted with ethyl acetate.

#### Raw data for standard curve

| TMTHF (ppm) | Retention time (min) | Area | Average Area | Decane (ppm) | retention time (min) | Average Decane |
| --- | --- | --- | --- | --- | --- | --- |
| 1622 | 3,094 | 207752,9 | 205612,6 | 5840 | 4,83 | 1076746 |
|  | 3,094 | 203030,8 |  |  | 4,829 |  |
|  | 3,101 | 206054,1 |  |  | 4,788 |  |
| 3244 | 3,068 | 373856,8 | 352406,2 | 5840 | 4,84 | 1003245 |
|  | 3,072 | 343289,6 |  |  | 4,833 |  |
|  | 3,076 | 340072,2 |  |  | 4,796 |  |
| 4866 | 3,039 | 563245,6 | 531417,7 | 5840 | 4,824 | 1075662 |
|  | 3,055 | 498578,9 |  |  | 4,805 |  |
|  | 3,059 | 532428,5 |  |  | 4,791 |  |
| 6488 | 3,02 | 779654,8 | 721617,3 | 5840 | 4,837 | 1067472 |
|  | 3,039 | 698409,7 |  |  | 4,806 |  |
|  | 3,041 | 686787,5 |  |  | 4,789 |  |
| 8110 | 3,016 | 939434,3 | 906225,2 | 5840 | 4,829 | 1068905 |
|  | 3,016 | 907274,1 |  |  | 4,806 |  |
|  | 3,022 | 871967,1 |  |  | 4,789 |  |
| 9732 | 3,001 | 1164111 | 1107938 | 5840 | 4,827 | 1156844 |
|  | 3,004 | 1070845 |  |  | 4,824 |  |
|  | 3,01 | 1088859 |  |  | 4,782 |  |

#### GC-FID standard curve

#### GC-FID Conversions calculations

Table 5: Example of descriptions and letters used for calculation of GC-FID conversions for TMTHF 1

| Letter | Description |
| --- | --- |
| A | Starting material mass (2,5-Dimethyl-2,5-hexanediol 2 ) in grams |
| B | Concentration in 50-100 mL sample |
| C | Concentration in 1 mL LC vail sample |
| D | Dilution factor |
| E | Area of product from GC-FID |
| F | Area/ Equation of product |
| G | F × Dilution factor |
| H | G / 1000 |
| I | H × Collected volume |
| J | % Conversion (I/ Expected product × 100 ) |

#### GC-FID Chromatograms

| Starting material: 2,5-Dimethyl-2,5-hexanediol 2 |  |
| --- | --- |
| Decane (Internal standard) and Starting material 2 |  |
| TMTHF 1 and Decane |  |
| TMTHF 1 (Zeolite batch product) used for standard curve generation |  |
| TMTHF 1 (200 gram before distillation) (90,8969% conversion, 9,1031% byproduct) |  |
| TMTHF 1 (200 gram after distillation) (99,9248% conversion, 0,0752% byproduct) |  |
| TMTHF 1 (Zeolite batch product and 200 gram flow reaction) |  |
| Byproducts |  |

## Characterization data

### Byproduct formation according to Byrne and co-workers1–5

| Byproduct (DHN) 2,5-dimethylhexa-2,4-diene 4 | Byproduct (DHN2) 2,5-dimethylhexa-1,5-diene 5 | Byproduct (DHN3) 2,5-dimethylhexa-1,4-diene 6 | Byproduct (HNL) 2,5-dimethylhex-4-en-2-ol 7 |
| --- | --- | --- | --- |

Figure 11: Predicted 1H-NMR spectra by Mestrenova of byproducts

### Nuclear magnetic resonance spectra

NMR 1: qNMR of batch reaction using H-beta zeolite as catalyst (97.02 % conversion using anisole as internal standard )

NMR 2: qNMR of batch reaction using citric acid monohydrate as catalyst (49.03 % conversion using anisole as internal standard)

NMR 3: qNMR of 200 gram flow reaction using citric acid monohydrate (94.16% conversion using anisole as internal standard)

NMR 4: 1H-NMR of batch reaction using H-beta zeolite as catalyst

NMR 5: 13C-NMR of batch reaction using H-beta zeolite as catalyst

NMR 6: DEPT 135 spectra of batch reaction using H-beta zeolite as catalyst

NMR 7: 1H-NMR of 200-gram flow reaction using citric acid monohydrate

NMR 8: 13C-NMR of 200-gram flow reaction using citric acid monohydrate

NMR 9: DEPT 135 spectra of 200-gram flow reaction using citric acid monohydrate

NMR 10: 1H-NMR of 2,5-Dimethyl-2,5-hexanediol 2 (Starting Material)

NMR 11: 13C-NMR of 2,5-Dimethyl-2,5-hexanediol 2 (Starting Material)

NMR 12: DEPT 135 spectra of 2,5-Dimethyl-2,5-hexanediol 2 (Starting Material)

### Fourier transform infrared spectra

Figure 12: IR spectrum of batch reaction using H-beta zeolite as catalyst

Figure 13: IR spectrum of 200-gram flow reaction using citric acid monohydrate

Figure 14: IR spectrum of 2,5-Dimethyl-2,5-hexanediol 2 (Starting Material)

### HRMS Spectra

Figure 15: HRMS spectrum of the 200-gram flow reaction using citric acid monohydrate

## References

1. 	F. Patrick Byrne, Greener solvents to replace toluene in the polymerisation and coating industry, PhD thesis, University of York (2017).

2. 	F. Byrne, B. Forier, G. Bossaert, C. Hoebers, T. J. Farmer, J. H. Clark and A. J. Hunt, 2,2,5,5-Tetramethyltetrahydrofuran (TMTHF): A non-polar, non-peroxide forming ether replacement for hazardous hydrocarbon solvents, Green Chem. 19 (2017) 3671–3678. DOI: 10.1039/C7GC01392B.