An in-situ FTIR-LCR meter technique to study the sensing mechanism of MnO2@ZIF-8/CNPs and a direct relationship between the sensitivity of the sensor and the rate of surface reaction

Lesego Malepe1, Patrick Ndungu2, Tantoh Derek Ndinteh1, Messai Adenew Mamo*1,3.

1Department of Chemical Science, University of Johannesburg, PO Box 17011, Doornfontein, 2028 Johannesburg, South Africa

2Department of Chemistry, University of Pretoria, Private Bag X20, Hatfield, 0028, Pretoria, South Africa

3 DST-NRF Centre of Excellence in Strong Materials (CoE-SM), University of the Witwatersrand, Johannesburg, Johannesburg, 2000, South Africa

Supporting document

Fig. S1: (a) A gold-plated interdigitated electrode and (b) a prepared sensor

Fig. S2: The SEM-EDS image of (a) CNPs, (b) MnO2 NRs, (c) MnO2@ZIF-8 and (d) MnO2@ZIF-8/CNPs

Table S1

| Sensing material | Analytes vapour | Sensitivity (Ωppm-1) |
| --- | --- | --- |
| MnO2 | methanol | -0.108 |
|  | ethanol | -0.119 |
|  | acetone | -0.0517 |
|  | Pentanone-3 | -0.0144 |
|  | diethylamine | -0.294 |
| CNPs MnO2@ZIF-8 MnO2/CNPs | Methanol Ethanol Acetone Pentanone-3 Diethylamine Methanol Ethanol Acetone Pentanone-3 Diethylamine Methanol Ethanol Acetone Pentanone-3 Diethylamine | 0.000607 0.00177 0.0001 0.00052 0.00289 -4.12 -2.98 0.196 -3.12 -1.18 0.0000912 -0.000035 0.00158 0.00993 0.00119 |

Dynamic response of MnO2-based sensor

Fig. S3: Dynamic response of MnO2-based sensor for (a & b) Acetone (c & d) Methanol (e & f) Ethanol (g & h) 3-pentanone (I & h) Diethylamine

Dynamic response of 1:1 mass ratio of MnO2@ZIF-8/CNPs based sensor

Fig. S4: Dynamic response of 1:1 mass ratio of MnO2@ZIF-8/CNPs based sensor for (a & b) Acetone (c & d) Methanol (e & f) Ethanol (g & h) 3-pentanone

Dynamic response of 2:1 mass ratio of MnO2@ZIF-8-CNPs based sensors

Fig. S5: Dynamic response of 2:1 mass ratio of MnO2@ZIF-8/CNPs based sensor for (a &b) Acetone (c & d) Methanol (e & f) Ethanol (g & h) 3-pentanone

Dynamic response of 3:1 mass ratio of MnO2@ZIF-8/CNPs based sensor

Fig. S6: Dynamic response of 3:1 mass ratio of MnO2@ZIF-8/CNPs based sensor for (a & b) Acetone (c & d) Methanol (e) Ethanol (f & g) 3-pentanone

Selectivity response

Fig. S7: Static response of 3:1 mass ratio of MnO2@ZIF-8/CNPs based sensor for mixed analyte